## Slide 1
Chart: EBF
No difference in edge vs. center elastic modulus
0 vs 20 minute time points – need more data
However, there is a clear difference in the properties over time (0 vs 40+ mins)
40+ min mineralized films seem to have a different shape (hyperelastic model?)
The stiffer the sample, the noisier the traces
Further 40, 90 min data impossible to process due to low contrast
Trial | Y. Modulus (kPa)
0-t1 | 40.4
0-t2 | 46.3
20-t1 | 25.7
40-t1 | 671.8
40-t2 | 491.5
60-t1 | 778.33
120-t1 | 3 Mpa

## Slide 2
Chart: Mineralization time (min)
| 0 | 0 | 20 | 40 | 40 | 60 | 120
 | 40.4 | 46.3 | 38.5 | 440 | 491.5 | 778.33 | 3000
No difference in edge vs. center elastic modulus
0 vs 20 minute time points – need more data
However, there is a clear difference in the properties over time (0 vs 40+ mins)
40+ min mineralized films seem to have a different shape (hyperelastic model?)
The stiffer the sample, the noisier the traces
Further 40, 90 min data impossible to process due to low contrast

## Slide 3
Chart: TBF
Differences between center and edge pieces, but not consistent
There might be a lot of heterogeneity within one biofilm or – small differences in thickness may lead to large differences in mineralization? (not sure – if this were the case, we should see that all center pieces are stiffer than edge pieces)
Needs a different model that considers yield stress/strain. I don’t think initial elastic modulus is the best feature to compare for these plots
20 min datasets failed but by 40 minutes, only the t1 dataset failed
Could not test 90+ min films because they were too brittle

## Slide 4
This plot may not be meaningful for TBF…
Chart: Mineralization time (mins)
| 20 | 20 | 40 | 40 | 40 | 60 | 60
 | 89.5 | 51 | 162 | 96.1 | 230.2 | 575.6 | 410.8
Trial | Y. Modulus (kPa)
20-t1 | 89.5
20-t2 | 51
40-t1 | 162
40-t2 | 96.1
40-t3 | 230.2
60-t1 | 575.6
60-t2 | 410.8

## Slide 5
Chart: QBF
Unfortunately these plots are too noisy 
Negative strain (compression) does not make sense
It is possible that a plate model rather than a membrane model would fix the issue – will try